Application of EcoStucco® products: Please refer to the product data sheets and specification guides for adequate preparation of the substrates and application methods.

DECOLIME – Architectural Lime Plaster to achieve a smooth and matte finish, emulating the texture of the fossil stone. The content of this bag mixes with 6.5 quarts of clean water. First blend the color (if any) with some of the mixing water. Mix DECOLIME to a heavy viscosity and let set for 10 minutes. Then remix to a workable, lump-free viscosity before applying. Add a controlled amount of water only if necessary. DECOLIME may also be used as a leveling coat, a base coat, or mesh coat.

Yields: 70 to 135 f²

UNILIME – Architectural Lime Plaster to achieve a pitted finish emulating the texture of limestone. Content mixes with 6.5 quarts of clean water. First blend the color (if any) with some of the mixing water. Mix UNILIME to a heavy viscosity and let set for 10 minutes. Then remix to a workable, lump-free viscosity before applying. Add a controlled amount of water only if necessary. UNILIME may also be used as a leveling, base, or mesh coat.

Yields 80 to 135 f²

TRADILAKT – Architectural Lime Plaster to achieve a moderately mottled, satin finish with minimal reflection, emulating the texture of a honed stone. Content mixes with 4.5 to 5 quarts of clean water. First blend color (if any) with some of the mixing water. Mix TRADILAKT to a heavy viscosity and let set for 10 minutes. Then remix to a workable, lump-free viscosity before applying. Add a controlled amount of water if necessary. TRADILAKT may also be used as a leveling, base, or mesh coat.

Yields: 70 to 100 f²

MURALIME – Architectural Lime Plaster to achieve a moderately mottled finish with low to high sheen, emulating the texture of marble. Content mixes with 4 to 5 liters (1 gallon) of clean water. First blend the color (if any) with some of the mixing water. Mix MURALIME to a heavy viscosity and let set for 10 minutes. Add a controlled amount of water based on chosen application method and remix to a workable, lump-free viscosity:

- Polished Plaster: add 1/2 qt. to 2 qt. | Yields 115 – 135 f²

- Velvety Plaster: add 2 qt. to 3 qt. | Yields 135 – 160 f²

- Lime Wash: add 6 to 8 qt. | Yields 270 – 400 f²

SHELF LIFE: Products are guaranteed for 12 months when stored in original package above ground and in normal conditions.

DRYING TIMES:  Dry to touch within 6 hours. Cured after 2 weeks or more under normal conditions, mix ratio, and ambient climate.  Optimal mechanical performances are reached within 6 months.

PRECAUTIONS: Avoid eye and skin contact. Wear protective eyewear and gloves to reduce risks of exposure. Use a respirator when mixing and sanding the material.

FIRST AID: Rinse affected area with fresh water immediately. If ingested, seek medical attention.

See Material Safety Data Sheet for further information.

www.ecostucco.com                                                   Please recycle (logo)