Description: Hardener for clear coat to be used with ULTRA clear coat. Hardeners are available in three speeds. Please choose the appropriate speed according to weather conditions.

| Speed | Temperature |
| --- | --- |
| Slow | 80°F-100°F |
| Medium | 68°F -80°F |
| Fast | 50°F -68°F |

DIRECTIONS:

1. Read all label directions, warnings and cautions on paint and catalyst.

2. Mixing Directions for Clear Coat with Activator:

2 Parts Clear

1 Part Activator

3. Adjust air pressure to 50-60 psi at the gun (siphon); 40-45 psi (gravity); 10 psi (HLVP).

4. Apply 2 full coats, allowing 10-15 minutes flash time between coats. Allow ample flash times.

5. When force drying, flash for 10-15 minutes, than force dry for 40 minutes at 140°F. Clear may be wet

sanded after 2-4 hours. Baking the clear will increase gloss.

6. Accelerator: Add 2 to 4 oz. can be added to a gallon of catalyzed clear to improve drying

times. Note that use of any Accelerator will shorten Pot Life and slightly reduce gloss. If an

Accelerator is added to EURO REFINISH Clear, it MUST also be added to the color.

7. Wet sand with 1500 grit or finer paper after 8 hours. Buff with appropriate compound.

8. Clean spray equipment immediately after use with lacquer thinner.

WARNING! FLAMMABLE,VAPOR AND SPRAY MIST HARMFUL.MAY CAUSE LUNG IRRITATION AND

ALLERGIC RESPIRATION REACTION: Keep away from heat, sparks and open flames. Isocyanates can

cause lung and skin sensitization and lung damage. Not to be used by persons who have lung or breathing problems or have reaction to isocyanates. Based on animal data, prolonged and repeated overexposure may cause adverse liver and kidney effects at various sites. Do not inhale vapors. Do not get in eyes, on skin or on clothing. Do not take internally. Use only in well ventilated areas. Wear appropriate, properly fitted NIOSH/MSHA approved respirator as directed by the manufacturer when airborne contaminate level(s) exceed exposure limits indicated in Section II of the MSDS. Select positive pressure supplied respirator TC-19C or equivalent) for isocyanates. Protect hands with impervious rubber gloves. Gloves must be checked before each use for signs of degradation, penetration and for proper functioning. Wear eye and face protection. Keep container closed when not in use. Since empty containers retain products residue and vapor, observe precautions even after container is empty. Subject to hazardous waste treatment storage and disposal requirements under RCRA. Incineration at EPA approved facility or dispose of in compliance with federal, state and local regulations. For further healthy and safety information and first aid, read the current Material Safety Data Sheet. Read warnings on individual labels before opening each container.

FIRST AID: In case of headache, dizziness, respiratory irritation or other systems of overexposure, move

from affected area and avoid further exposure. If symptoms persist, contact physician immediately. In case of skin contact, wash skin thoroughly with hand cleaner followed by soap and water. If irritation, rash or other disorders develop, get medical attention immediately. In case of eye contact flush eyes with running water for at least 15 minutes and get medical attention immediately. If ingested, contact physician immediately.

NOTICE: Reports have associated repeated and prolonged occupational overexposure to solvents with

permanent brain and nervous system damage. Intentional misuse by deliberately concentration and inhaling this product may be harmful or fatal.

Proposition 65 Statement: WARNING! This product contains a chemical known to the state of California

to cause cancer, birth defects or other reproductive harm.

KEEP OUT OF THE REACH OF CHILDREN

For professional use only by trained and qualified paint personnel using all proper safety equipment and application techniques

Contents: Xylene CAS# 1330-20-7, Acetone CAS# 67-64-1, Butyl Acetate CAS# 123-86-4,

2-Methoxy-1-Methyl Ethyl Acetate CAS# 108-65-6, Ethyl Benzene CAS# 100-41-4

EMERGENCY TELEPHONE NUMBER: CHEMTREC U.S 1-800-424-9300

Sprayable:  2.1 lbs/gal VOC

FOR SALE ONLY BY PROFESSIONALS.

NOT FOR SALE TO OR USE BY GENERAL PUBLIC

Notice to purchaser: Limited Warranty. The

following is made in lieu of all express or implied

rights, warranties and conditions. All

goods are manufactured of first class materials.

Neither seller nor manufacturer has control

over the use and application of the product.

It is the responsibility of the purchaser to determine

the suitability of the product for its intended

use. The liability of the seller and

manufacturer shall not exceed the purchaser

price of the product.

WARNING: FLAMMABLE LIQUID AND VAPOR.

VAPORS AND SPRAY MIST HARMFUL IF INHALED.

MAY CAUSE CENTRAL NERVOUS SYSTEM EFFECTS

SUCH AS DIZZINESS, HEADACHE OR

NAUSEA. MAY CAUSE NOSE, THROAT, EYE AND

SKIN IRRITATION. (FOLLOW ALL DIRECTIONS

AND CAUTIONS ON BACK PANEL)

WARRANTY: The recommendations for application of

this product are based on data obtained by our own research

facilities and is believed accurate. The manufacturer

warrants all material sold by it against defects in

the material but does not warrant its fitness for any specific

application use. The manufacturer makes no other

warranty of this material express or implied. This product

is intended to be used solely by professionally

trained personnel using proper equipment.