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Figure 3. Biofims formed on ETT segments (5 mm) ofte the ndicated number of days ofincubation (dily exchange of growth medium and re-in
ocuiotion). Measurements were made in ipicate. Black bors, uncooted tube segments; ey bars, coated segments. (o) MRSA (BAA-41, 10° cfu in-
oculotion. (8) K. pneumoniae (ATCC 13883, 10° cfu inoculation. () P. aeruginesa (ATCC 47085, 10° cu inoculatin). (d) . lbicans (ATCC 50028,
10° cfuinseulation).(e) C.auris (CDC 0383, 10°cunoculation.
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Figure 3. Biofims formed on ETT segments (5 mm) ofte the ndicated number of days ofincubation (dily exchange of growth medium and re-in
ocuiotion). Measurements were made in ipicate. Black bors, uncooted tube segments; ey bars, coated segments. (o) MRSA (BAA-41, 10° cfu in-
oculotion. (8) K. pneumoniae (ATCC 13883, 10° cfu inoculation. () P. aeruginesa (ATCC 47085, 10° cu inoculatin). (d) . lbicans (ATCC 50028,
10° cfuinseulation).(e) C.auris (CDC 0383, 10°cunoculation.
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Figure 4. Mixed species biofims formed on ETT segments (5 mim) afte the indicated number of days of incubation (dally exchange of growth me-
dium and re-inoculaton). Measurements mode in iplicate. Black bors: uncoated tube segments; gray bars: coated segments. (a) MRSA (BAA-41,
10°cfu inoculation) with P. oeruginosa (ATCC 47085, 10% cfu inoculation. (5) P. ceruginosa (ATCC 47085, 10° cfu inoculation) with C. ouris (CDC 0383,
10° cfu inoculation).
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Figure 5. SEM images of ET surfaces. () Bofim of C.auris (CDC 383) on on uncoated tube after 14 days (daily inoculation. (8) Surface of  cooted
tube after 14 doys (daily inoculation with C. auri). c) Mixed species biofim of MRSA and PAD] on an uncoated tube after 48 (¢)Surface of  coated
tube after 48k (ioculation with MRSA and PAOL). ¢) Mixed species biofilm of PAO1 and C.auris on an uncoated tube after 48K () Surface of a coated
tube ofter 48k (inoculation with PAOY ond C. auris)
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Figure 6. Quantifiation of the amounts of endotoxin in the growth medium and on ETT segments after incubtion with P. aerugingsa for the indi
cated time periods. Black bars, uncoated tube segments. Grey bars, cooted tube segments.




