## Slide 1
AISHI Aluminium Cap
M-Lead Type vs V chip Type
Proprietary and Confidential – Do not distribute without written permission
COPYRIGHT © 2018 The Hunan Aihua Group, Ltd. ALL RIGHTS RESERVED

## Slide 2
Cost Advantage
M-Leaded vs Radial Leaded vs V-Chip
M Type
V Chip
With the improvement of automation level and labor costs, there are more and more SMD products, but the price of SMD products is still much higher than that of conventional products. Aishi group has been considering to reduce costs for customers and achieve a win-win situation.
V-chip. M-Type

## Slide 3
Advantage of better Solder-Reflow Ability and lower cold soldering rate
M-lead vs V Chip
Temp. of Can | V-Chip | M-lead
Max ℃ | 236.67 | 228.06
Solder-Reflow Ability | Good | Excellent
Comparison data of Reflow chart of Al Can Temp.
M-leaded type SMD Al cap is a lower reflow temperature, which improved the solder quality, lower the cold soldering rate and easier to be reworked.

## Slide 4
Extent the Lifetime of Al cap by M-lead
Lx = Lo ×2（To-Tx)/10 × 2(△To-△Tx)/5
12W 25℃ | Test Point(℃) | 0.5H | 1H | 2H | 3H
M-Lead SMD | Top | 93.2 | 94.6 | 94.5 | 94.6
 | Side | 97.1 | 98.5 | 98.4 | 98.5
V-Chip SMD | Top | 101.9 | 103.6 | 103.7 | 103.8
 | Side | 104.4 | 106.1 | 106.2 | 106.3
Application Analysis of LED Lighting
When using on al-based PCB, temp. on M-leaded type Al cap will be 5 - 8 ℃ in average, which will lead to longer lifetime of M-leaded type.
Electric Parameter |  |  |  |  |  |  |  | Temp |  |  | Lifetime Calculation | 
Series | WV(V) | Cap Value （uF） | Diameter （mm） | Height （mm） | Lo Rated Lifetime(H) | Io Rated RC (mA) | To Rated Temp. (C) | Tc(Al Can) | Tx(Ambient) | Temp. Rise | Lx(hrs) | Lx(year)
MF SMD Type | 400 | 3.3 | 8 | 10.5 | 6000 | 72 | 105 | 103.8 | 103.45 | 0.39 | 12666 | 1.45
MF M-leaded | 400 | 3.3 | 8 | 10.5 | 6000 | 72 | 105 | 94.6 | 94.25 | 0.39 | 23965 | 2.74

## Slide 5
LC Characteristics comparison before and after M-leaded
Characteristics Comparison
Little change of cap value before and after M-leaded, LC changes within which is allowed.
NOT ENOUGH INORMATION
What is X axis??? What is before and after mean?????

## Slide 6
Inner Structure comparison before and after M-leaded
CT Capture of Inner Structure
MH 400V4.7 8*13.5
Before
After
MF 400V3.3 8*10.5
There is no obvious change of inner structure，no inner damage before and after M-leaded manufacturing process

## Slide 7
Item | V-Chip | M-Leaded
Cost | higher | Lower
Electrical Performance | Excellent | Excellent
Manufacturing Process | Forming by radial Plate Tape and Reel | Forming by radial Tape and Reel
Lifetime | Normal | Longer
Cold Soldering | Normal | Lower
Rework | Hard | Easy
Ripple Current | High | High
Characteristics Summary between M-leaded and V-Chip

## Slide 8
Thank You For Being Our Trusted Partner.
THANK YOU