Absorbacide Mineral Analysis
Organics Made Easy Absorbacide contains these minerals:

Silicon Dioxide (SiO2)
  
90.10%

Phosphorus Pentoxide (P2O5) 
0.03%

Aluminium Oxide (Al2O3)
4.62% 

Titanium Dioxide (TiO2) 

0.37%

Iron Oxide (Fe2O3)

 3.16% 

Vanadium Oxide (V2O5)

 0.03%

Manganese Oxide (MnO)
 0.02% 

Chromium Oxide (Cr2O3)
 0.005%

Magnesium Oxide (MgO )
0.56%

Copper Oxide (CuO)

 0.004%

Calcium Oxide (CaO)

 0.62% 

Zinc Oxide (ZnO)

 0.007%

Sodium Oxide (Na2O)

 0.11%

Potassium Oxide (K2O)

 0.06%

Sulphur Trixode (SO3)

 0.06%

Chlorine (Cl)


 0.05%
